R&D/FCL/2503/PF/75                                                                                        Date: 24-03-2025

RECEIVED FROM: Mr. Santhosh

CUSTOMER           : -

FABRIC TYPE       : 100% Polyester Garment fabric (Light Green & Orange Shade)

TESTED FOR        :  To remove the polyester dyes stain from garment

_________________________________________________________________________________________________________

Application:

| Substrate – 100% Polyester Garment fabric (Light Green & Orange Shade) |  |  |
| --- | --- | --- |
| Process - By Exhaust Method (Stain Removal) |  |  |
| Sr. No | Product Name | Recipe |
| 1 | Finocon SR New | 1% |
| 2 | Finocon DON | 1% |
| 3 | Finocon WS Powder | 1% |
| PARAMETERS |  | Temp-80 ºC 30 min |

Observation:-

- 100% Polyester Garment (Light Green Shade)

(1)

| Before Treatment Sample | After Treatment sample |
| --- | --- |

(2)

| Before Treatment Sample | After Treatment sample |
| --- | --- |

(3)

| Before Treatment Sample | After Treatment sample |
| --- | --- |

.

- 100% Polyester Garment (Orange Shade)

(1)

| Before Treatment Sample | After Treatment sample |
| --- | --- |

| Before Treatment Sample | After Treatment sample |
| --- | --- |

(2)

(3)

| Before Treatment Sample | After Treatment sample |
| --- | --- |

- 100% Polyester Garment (Light Green & Orange Shade)

Remark:

Removal of stain is observed by using above recipe.

COMMENTS:

Prepared By                                                                                           Authorized By

Afreed Mujawar	                                                                                    Purva Rane

(Lab Chemist-R&D Textile)			                                 (Manager- R& D Textile)